## Slide 1: Code and Standards Requirements For Acceptance Testing
NRMCA

## Slide 2: Disclaimer
This presentation has been prepared solely for information purposes. It is intended solely for the use of professional personnel, competent to evaluate the significance and limitations of its content, and who will accept full responsibility for the application of the material it contains. The National Ready Mixed Concrete Association and any other organizations cooperating in the preparation of this presentation strive for accuracy but disclaim any and all responsibility for application of the stated principles or for the accuracy of the content or sources and shall not be liable for any loss or damage arising from reliance on or use of any content or principles contained in this presentation. Unless otherwise indicated, all materials in this presentation are copyrighted to the National Ready Mixed Concrete Association. All rights reserved. Therefore reproduction, modification or retransmission in any form is strictly prohibited without the prior written permission of the National Ready Mixed Concrete Association. © 2008 National Ready Mixed Concrete Association.

## Slide 3: Acceptance Testing (defined)
test, acceptance, n (ASTM C125) —a test performed to determine whether an individual lot of a product conforms to specified requirements
Architect/Engineer specifies 4000 psi
Sampling and testing to comply with standards
  1 cu.ft. sample represents 10 cubic yards OR 150 cyds
Improper procedures generate inaccurate results
  High costs and delays
Notes: Testing is performed on deliveries of concrete to determine whether the quality of concrete supplied meets the requirement of the specification. Any concrete structure that is built in accordance with the Building Code, state transportation or other public agencies will require that concrete be tested, typically by a third party testing agency that is hired by the owner or owner’s representative.
The sample of concrete obtained is rather small compared to the volume of concrete represented. Typically a 1 cubic foot sample is obtained from a truck mixer that may contain 10 cubic yards (about 4% of the load). Typically one sample is taken for every 100 or 150 cubic yards – 10 or 15 loads of concrete. So the test results obtained from that 1 cubic foot sample will represent the quality of that volume of concrete. If the results do not meet the requirements of the specification, this renders that this volume of concrete might be of questionable quality. Some of it will be placed in the structure. The cost of concrete represented by a series of tests performed on one sample of concrete is between $1000-2000 per load or between $15,000 to $30,000 for 15 loads.
It is important that the testing agencies performing tests on concrete comply with the procedures applicable in the standards. Any deviation from these procedures will generate erroneous results that might penalize acceptable concrete. This evaluation will incur significant costs to several entities and will delay the completion of the project – this causes revenue loss to the owner of the structure.

## Slide 4: Scope of Testing
Samples obtained in accordance with ASTM C172
  Point of delivery from transportation unit (or mixer)
  Other sampling methods should be defined
Fresh Concrete tests
  Slump or slump flow – tolerances in ASTM C94; ACI 117
  Air content – tolerance ±1.5%
  Temperature – limits in specifications
  Density – typically no limits unless its lightweight concrete
  Strength specimens
    Average of two 6x12 in or three 4x8 in cylindrical specimens
    Standard cured in accordance with ASTM C31
    Tested in accordance with ASTM C39 at 28 days or as per spec
Notes: There are consistent details on how sampling and testing needs to be performed. These are addressed in the building code, reference and project specifications, specification for ready mixed concrete and in the contract with the testing agency.
Sampling is the first important step. The sample obtained must be representative of the load. This is assured when the procedure of obtaining a sample is in accordance with ASTM C172 – middle portion of the load with two or more portions of the discharged concrete mixed together to create a composite sample. ASTM C172 only describes sampling from the transportation unit. Often, project specifications will require tests to be performed on samples obtained at the point of placement in the structure – at the end of a bucket, pump, etc. Sampling at this location is not described in ASTM C172, so the procedure has to be clear. The problem is that the characteristics of the concrete can change by the procedure used to convey it from the truck discharge to the point of placement. The concrete supplier has no control on this process, cannot anticipate the types of changes that might occur and thereby cannot be responsible for tests results at the point of placement. These issues should be discussed at a pre-construction conference. More information about this can be found at http://www.nrmca.org/research_engineering/RMC_Specs_Guide.htm.
Typically several fresh concrete tests are performed as listed on the slide. Most of these tests have specification criteria that should be met, with stated or industry-established tolerances.
Additionally specimens for tests on hardened concrete are also prepared, typically strength tests. There are detailed requirements on making and curing these specimens up to the point they are tested.

## Slide 5: Standard Curing Vs Field Curing
Removal of forms or shoring
Minimum strength for post-tensioning
Determine if structure can be put into service
Adequacy of curing and protection
Compare with standard cured or with other in-place tests
Quality control
Checking adequacy of mixture proportions for strength
Acceptance testing for specified strength
Notes: Specimens for strength testing are prepared and cured in accordance with ASTM C31. There are two distinct curing procedures described in ASTM C31 – standard curing and field curing. These different curing methods are used depending on the purpose of the test results. These reasons are shown on the screen as summarized from C31.
Specimens for strength tests to determine the quality of concrete supplied to a project should follow the standard curing procedure. This is clear in the industry standards. There is a misconception, even by practicing engineers that the purpose of the tests are to determine the strength of concrete in the structure and thereby specimens should be field-cured. This is incorrect.

## Slide 6: ACI Strength Acceptance Criteria
Test results - Should meet both criteria
1. Average of 3 consecutive  ´c
2. Single test  (´c – 500)
  For ´c > 5000 psi – Single test  0.9´c
Notes: To reiterate, acceptance of concrete is based on samples of concrete obtained in accordance with ASTM C 172, test specimens prepared and cured in accordance with ASTM C 31, and tested in accordance with ASTM C 39. The test age for cylinder strengths is 28 days or as required by the job specification. Once the mix is approved and the job has started, the tests of laboratory-cured specimens made from the job concrete must satisfy both of the following requirements before the concrete is considered acceptable:
1. The average of all sets of three consecutive strength tests equal or exceed the specified strength (ƒ´c).
2. No single strength test (average of 2 cylinders) falls below the specified strength (ƒ´c) by more than 500 psi [3.5 MPa] or 10% of ƒ´c when the specified strength exceeds 5000 psi (35 MPa).

## Slide 7: ACI 318-19 for Low Strength Results
Avg 3 consecutive - less than ´c
  Increase strength level
Single test - less than (´c - 500)
  Increase strength level
  Investigate low strength - structural safety
    Reduced load carrying capacity of structure confirmed by calculations
    Core tests
Notes: If either of the criteria are not met, the code indicates that steps should be taken to increase the level of subsequent test results. The commentary recommends these measures:
Increase the cementitious materials content
Change the mixture proportions
Reduce or have better control on the slump level supplied
Shorten the delivery time
Closer attention to the air content
Evaluate the quality of testing to ensure that the standards are being complied with.
If the single test is more than 500 psi less than the specified strength (2nd criteria), the code also requires that an investigation of low strength test results be followed. The low strength result should be a cause for concern on whether the structural capacity of the region represented by the low strength is adequate. This is a public safety issue.

## Slide 8: Field Cured Cylinders
For evaluating protection and curing of structure (ACI 318)
  Acceptable if field cured cylinders
  > 85% of companion lab cured
  Or
  > (´c+ 500) psi
Also used for formwork removal, post-tensioning…
Notes: ACI 318 has a specific purpose for using strength test results from field-cured cylinders – for evaluating the protection and curing afforded to the structure. There are criteria for strength tests from field cured cylinders as indicated on the slide.
These tests are also used for other purposes to estimate the strength of concrete in the structure.

## Slide 9: Requirements for Laboratories
ACI 318
ACI 301
1.7.3.1 Owner’s testing agencies that perform required
tests of concrete materials will meet the requirements of
ASTM C1077, which includes certification requirements
for technicians. Owner’s testing agencies that test or inspect
placement of reinforcement will meet the requirements of
ASTM E329.
1.7.2.1 Field technicians—Field tests of concrete required
in 1.7.2 shall be performed by ACI Concrete Field Testing
Technician Grade I or acceptable equivalent.
1.7.3.2(c) Owner’s testing agency will report test and
inspection results of Work to Owner, Architect/Engineer,
Contractor, and concrete supplier within 7 days after tests
and inspections are performed. Strength test reports will
include location in Work where concrete represented by
each strength test was deposited, date and time sample was
obtained, and batch ticket number. Strength test reports will
include information on storage and curing of specimens
before testing.
Notes: TEST REPORTS NOT SENT IS A HUGE ISSUE
These are excerpts from ACI 318 and ACI 301 regarding requirements for testing agencies and technicians.
ASTM Standard Practice C1077 identifies and defines duties, responsibilities and minimum technical requirements of testing laboratories’ personnel and minimum technical requirements for laboratory equipment utilized in testing concrete and concrete aggregates. The standard also provides criteria for the evaluation of capabilities of testing laboratory to perform ASTM test methods for accreditation purposes. This practice requires laboratories to have ACI certified or equivalent field testing technicians as well as certified strength testing technicians. Supervisory personnel must have at least three years of relevant experience and hold current certification.
ACI 318 states that labs should share test data with all stakeholders. ACI 301 Section 1.6.3.1.c states that labs should share test data within 7 days of completion of test.
ACI 301 also states that strength test reports should include information on storage and curing of test specimens before testing.

## Slide 10: Quality Assurance
Testing Lab conducting QA testing
Conformance to ASTM C1077
  Inspected
  Accredited
Technicians Certified
  Field Testing
  Strength Testing
  Lab Testing
Testing in accordance with ASTM or AASHTO
Timely distribution of test reports to all parties
Notes: This slide summarizes the requirements for testing agencies.
Conform to ASTM C1077 – the labs may need to be accredited – which requires inspection and documentation of corrective action of deficiencies resulting from the inspection.
Technicians in the field and lab have to be certified.
Tests should be performed in accordance with the standards.
It is also important that all test reports be distributed to all parties that are impacted in a timely manner. Only if the producer is provided with all test results can he take action to avoid failing test results.

## Slide 11: Laboratories – ASTM C1077
Quality System
  Written manual
  Under direction of PE
  Personnel evaluation
  Equipment calibration
  Inventory control
  Participation in proficiency sample program
  Laboratory inspection and accreditation
Notes: A laboratory testing concrete in accordance with ASTM C1077 must maintain a written Quality System. This internal quality assurance system requires laboratories to maintain and calibrate equipment on a regularly scheduled basis. The lab must have a system in place to address technical complaints. The laboratory must participate in a proficiency testing program such as CCRL Concrete Proficiency Sample Program or the AMRL Aggregate Proficiency Sample Program.

## Slide 12: Factors Affecting Strength
Notes: This comprehensive paper by Richardson quantifies various factors that will negatively impact the strength test results of concrete specimens – both for procedures in the laboratory and the field. All these factors are cumulative. This paper is available from the NRMCA.

## Slide 13: Frequent violations - Testing
Reason (Average strength reduction)
Initial curing (30%)
Damaging “green” specimens (18%)
Filling in one layer (17%)
From chute / no tapping (12%)
Top etching / no lids (11%)
Adapted from Snell
Notes: This is a summary of observations from Luke Snell on more common violations on specimen preparation and care at the jobsite – and the impact on strength reduction. Initial curing can amount to up to 30% reduction in strength by his assessment.

## Slide 14: Frequent violations - Testing
Notes: These are some images on jobsite issues – using a rebar, improper consolidation, improper filling the cylinder, not finishing the surface properly and improper initial curing at the jobsite.

## Slide 15: Acceptance of concrete
ACI 318-19 Section 26.12.1.1
26.12.1.1 Compliance requirements:
(a) Evaluation of hardened concrete shall be based on strength tests. A strength test is the average of the compressive strengths of at least two 6 x 12 in. cylinders or at least three 4 x 8 in. cylinders made from the same sample of concrete taken in accordance with ASTM C172 at the point of delivery, handled and standard-cured in accordance with ASTM C31, and tested in accordance with ASTM C39 at 28 days or at test age designated for fc′.
Notes: ACI 318-19 clearly states that for acceptance of concrete supplied by the concrete producer, cylinders shall be standard cured in accordance with C31

## Slide 16: Strength Test Specimens
Standard Curing - ASTM C31
Maintain moisture
Initial temperature in field
  60°F to 80°F
  ƒ´c > 6000 psi - 68°F to 78°F
Transport to lab within 48 hrs
Transportation time 4 hrs or less
Lab curing 73.5±3.5°F and moist
Notes: This slide summarizes the details regarding standard curing of test specimens as stated in C31.
An important factor is the proper maintenance of moisture and temperature during the first 24-48 hours in the field. This tends to be the biggest observed violation that impacts strength test results used for acceptance of concrete.

## Slide 17: Strength Test Specimens
Standard Curing - ASTM C31
Maintain moisture
Initial temperature in field
  60°F to 80°F
  ƒ´c > 6000 psi - 68°F to 78°F
Transport to lab within 48 hrs or 8h after final set
Transportation time 4 hrs or less
  Proper Cushioning, Protect from Freezing, Moisture Loss
Lab curing 73.5±3.5°F and moist
Notes: This slide summarizes the details regarding standard curing of test specimens as stated in C31.
An important factor is the proper maintenance of moisture and temperature during the first 24-48 hours in the field. This tends to be the biggest observed violation that impacts strength test results used for acceptance of concrete.
Upon completion of initial curing, cylinders should be transported to the laboratory for final curing within 48 hours after they were cast but at least 8 hours after final set. Specimens are generally only 24 hours old at this point and are very susceptible to damage if mishandled.
Specimens should be moved carefully and should be kept in their molds until they reach the laboratory.
Always ensure that caps or plastic bags remain on the specimens during transportation to ensure that there is no loss of moisture from the specimens.

## Slide 18: ASTM C31 Note 14 – Standard Curing
Satisfactory moisture environment
Immerse in water with lids
Store in container or enclosure
Place in damp sand pits
Cover with removable lids
Place inside plastic bags
Cover with wet fabric
Notes: ASTM C31 provides some guidance on methods that can be used to maintain the moisture and temperature environment for the initial curing of test specimens
These are suggestions for maintaining a satisfactory moisture environment.

## Slide 19: ASTM C31 Note 12 – Standard Curing
Satisfactory temperature environment can be created by the use of
Ventilation
Ice
Cooling devices
Heating devices - electrical heaters or bulbs
Immersion in water may be easiest to control temperature
Notes: These are suggestions for maintaining a satisfactory temperature environment
It is suggested that the best way to maintain both temperature and moisture environment is to immerse the cylinders in water for the initial curing period. Studies have shown that this achieves the highest strength of concrete compared to other curing methods.

## Slide 20: Violation of standard procedures
Initial Curing is the most frequent problem
Notes: Some examples of unacceptable initial curing procedures in the field

## Slide 21
Colorado Ready Mixed Concrete Assn. – CTAC program
Notes: The Colorado Ready Mixed Concrete Association initiated a program whereby individuals would observe various details on compliance with testing procedures at project sites. This summary for August and through August indicate that only about one-third of the time was initial curing of test specimens done correctly.
The green line indicates compliance and the red line indicates non-compliance in all questions. For question 4, there are many different forms of non-compliance.

## Slide 22: ASTM C31 – Report
12. Report
12.1 Report the following information to the laboratory that will test the specimens:
12.1.1 Specimen identification,
12.1.2 Serial number of delivery ticket, if available,
12.1.3 Location of concrete represented by the samples,
12.1.4 Date, time and name of individual molding specimens,
12.1.5 Slump or slump flow, air content, and concrete temperature, test results and results of any other tests on the fresh concrete, and any deviations from referenced standard test methods, and
12.1.6 Curing method. For standard curing method, report the initial curing method with maximum and minimum temperatures and final curing method. For field curing method, report the location where stored, manner of protection from the elements, temperature and moisture environment, and time of removal from molds.
Notes: These are the reporting requirements in ASTM C31.
The reporting section of ASTM C31 states that for standard curing, the initial curing method with maximum and minimum temperatures should be reported to the entity testing the cylinders. However, this is seldom, if ever, seen on a strength test report (which complies with the reporting requirements of ASTM C39).
Most reports will have some statement that the making and curing of specimens complied with ASTM C31 with no detail.

## Slide 23: Statements in Laboratory Reports
Notes: These are typical statements regarding conformance with ASTM C31 extracted from different strength test reports. There is no information about the max and min temperatures during the initial curing in the field

## Slide 24: Initial Curing
CTAC Observations says <50% follow C31
Concrete test reports don’t report max min temps. during initial curing
Are Code requirements for C31 being followed?
So what?
Notes: In Note 8, ASTM C31 provides some guidance on methods that can be used to maintain the moisture and temperature environment for the initial curing of test specimens
These are suggestions for maintaining a satisfactory moisture environment.

## Slide 25: Effect of non-standard initial Curing
Initial Curing Conditions | Strength loss at 28 days Relative to Standard Curing, %
3 days at 100°F and 25% RH(lab)1,2 | 22
24 h at 71°F to 107°F (outdoors sunlight New Mexico)3 | 15
48 h at 72°F to 89°F (outdoors covered 5-gal bucket Maryland)4 | 22
48 h at 20°F to 34°F (outdoors covered 5-gal bucket Maryland)4 | 22
22 hours at 80°F in air (lab)5 | 16
24 hours at 67°F to 93°F (outdoors in sunlight Colorado)6 | 28
24 to 48 hours at 90°F in water (lab)7 | Up to 20
Notes: Obla, K.H., Werner, O., Hausfeld, J.L., MacDonald, K.M., Moody, G.M., and Carino, N.J., “Who is Watching out for the Cylinders,” Concrete International, V. 40, No. 8, 2018, pp. 28-35.
Bloem, D.L., “Effect of Curing Condition on Compressive Strength of Concrete Test Specimens,” NSGA Circular No. 59 and NRMCA Publication No. 53, 1954, 15 pp.
Montoya, R., “Hot Weather Comparison Program – Fresh Concrete Testing and Initial Curing Practices,” Report to General Membership, New Mexico Ready Mix Concrete and Aggregates Association, Albuquerque, NM, Apr. 1995, 11 pp.
Obla, K.H.; Rodriguez, F.; and Ben-Barka, S., “Effects on Non-Standard Curing on Strength of Concrete: A Research Project at the NRMCA Research Laboratory – Series D 335 and D 338,” Concrete in Focus, V. 3, No. 4, Winter 2005, pp. 57-59.
Meininger, R., “Effects of Initial Field Curing on Standard 28-Day Cylinder Strengths,” Cement, Concrete, and Aggregates, V. 5, No. 2, 1983, pp. 137-141.
Kane, K.; Laker, T.; and Morrical, S., “Improving the Quality of Concrete Testing,” Concrete International, V. 37, No. 8, Aug. 2015, pp. 33-40.
White J.L., Fleming K.R., and Schindler A.K., 2023, “Evaluation of jobsite cylinder curing practices for the Alabama concrete industry,” ALDOT Project 931-051, Final Research Report, Highway Research Center, Auburn University, Alabama, 179 pages, https://eng.auburn.edu/research/centers/hrc/research/final-reports, Accessed February 2, 2024.
Alabama work is for 8 mixes. RH was not varied.

## Slide 26: Effects of Initial Curing
Importance of temperature and duration of initial curing on 28-day compressive strength
NRMCA Pub 53; Delmar L. Bloem,1954
Initial curing conditions | Relative 28-day strength, %* |  | 
Temperature | 37°F at 100% RH | 73°F at 60% RH | 100°F at 25% RH
1 day in air | 100 | 92 | 88
3 days in air | 93 | 89 | 78
*In comparison with compressive strength of 5590 psi determined for specimens moist cured at 73°F and 100% RH
Notes: This is a portion of a larger NRMCA study conducted in the 1950s. The data shown are for a concrete mixture proportioned with ordinary portland cement at 517 lb/yd3 (307 kg/m3), w/c of 0.57, and a 3 to 4 in. (75 to 100 mm) slump.
The comparison is based on cylinders that were moist cured soon after casting (representing the 100% strength of 5590 psi)
6x12 in. Specimens were molded at 73°F, subjected to initial curing conditions in air at temp and RH, age as stated, and transferred to standard moist room at 73°F for curing until test age of 28 days.
Specimens initially cured in air for 1 day at 37, 73, and 100°F achieved 100, 92, and 88%, respectively, of the strength of specimens that were moist cured at 73°F from the time of molding until testing (5590 psi or 38.5 MPa). Specimens initially cured in air for 3 days at 37, 73, and 100°F achieved 93, 89, and 78% of the strength of specimens that were moist cured at 73°F from the time of molding until testing, respectively.
While there was no apparent strength reduction associated with initial curing in air at 37°F (3°C) Bloem5 noted that low initial curing temperatures in the field could be accompanied by a lower RH than was present in the reported study, which could be expected to reduce the 28-day strength.

## Slide 27: Effects of Initial Curing
Importance of temperature and moisture during first 24 hours of initial curing – on 28-day compressive strength
4860 psi
Montoya – New Mexico, 1995
Type of 1-day initial curing | Temp. range, °F | Relative strength, %
Outdoor exposure: curing box with thermostatic control; in water | 71 – 76 | 100
Laboratory: immersed in lime water (control) | 76 – 82 | 100
Laboratory: in air | 78 – 82 | 88
Outdoor exposure to sunlight: not protected | 71 – 107 | 85
Outdoor exposure: covered with wet burlap and plastic | 94 - 140 | 83
Specimens molded at 86°F at the jobsite and subjected to the initial curing condition for 24 h
Notes: Study done by the NM ready mixed association in 1995
In this case the importance of ensuring that the cylinders are kept moist during the initial curing period is also illustrated.
Concrete was mixed in a truck and had a slump of 3-3/4 in. (95 mm), air content of 5.8%, and fresh concrete temperature of 86°F (30°C).
Cylindrical specimens (6 by 12 in.) were molded and stored initially for 24 h under five different conditions as shown in Table 3. Specimens were covered with plastic lids.
At the end of the initial curing period, specimens were transferred to a standard moist room at 73°F until the test age of 28 days.
Cylinders that were kept in air in a lab environment but not immersed in water had a 12% lower strength.
specimens immersed in water inside a thermostatically controlled curing box on site attained strengths comparable to control specimens immersed in water in the laboratory (see Fig. 3).
They also show that specimens exposed to ambient conditions without temperature control exhibited strength reductions of 15 and 17% relative to control specimens.
Montoya7 questioned whether any initial curing method that does not involve immersion in water would be acceptable in all RH conditions.

## Slide 28: Effects of Initial Curing
Initial curing for 24 hours - Within limits of ASTM C31
NRMCA study: Meininger, ASTM Cement Concrete & Aggregates, 1983
Average Effect:
Water vs. Air +6.6%
60°F vs. 80°F +9.2%
60°F water vs. 80°F air +16%
Both temperature limits and moisture provision matter
Initial curing condition† | Relative 28-day strength, % | 
 | Cement A | Cement B
60°F in water | 100% (6080 psi) | 100% (6090 psi)
60°F in air | 92 | 97
80°F in water | 89 | 93
80°F in air | 81 | 88
Specimens molded at 73°F, subjected to initial curing condition for 22 h, and transferred to standard moist room at 73°F for curing until test age of 28 days
Notes: This is an NRMCA study published by Rick Meininger in 1983. It illustrates the difference in strengths even when cylinders are maintained within the temperature and moisture conditions applicable to ASTM C31.
The concrete mixture was proportioned with ordinary portland cement from two different sources (cement A and B) at 580 lb/yd3 (344 kg/m3), w/c of 0.51, and a 3 to 5 in. (75 to 125 mm) slump.
Cylindrical specimens (6 by 12 in.) were molded at room temperature (70 to 72°F [21 to 22°C]) and initially cured as shown for 22 hours.
The specimens stored in air were placed in plastic bags and sealed with rubber bands, while the water-immersed specimens were not covered.
At the end of the initial curing period, specimens were transferred to a standard moist room at 73°F until the test age of 28 days. B
Both 60°F and 80°F initial curing for 22 hours in air resulted in 3 to 8% (avg. 6.6%) lower strengths compared with initial curing under water.
Initial curing at 80°F resulted in 7 to 11% (avg. 9.2%) lower strengths compared with initial curing at 60°F as long as the moisture conditions were not varied.
Initial curing at 80°F in air resulted in 12 to 19% (avg. 16%) lower strength compared with initial curing at 60°F in water.
The specimens cured initially under water had a lower temperature rise compared with the specimens stored initially in air. This was also observed in the 1954 study. For specimens initially stored in air, the temperature increase for specimens made with cement A was greater than for specimens made with cement B. This explains the greater strength reductions in the specimens made with cement A. Meininger6 also found that specimens with 2 days of initial curing exhibited strength reductions that were nearly the same as specimens with 1 day of initial curing.
These studies show that both temperature limits and ensuring that cylinders are immersed in water matter to the strength.

## Slide 29: Effect of non-standard initial Curing
20% compressive strength loss
Variations in strength – higher standard deviations
Producer must increase their strength over-design
  Above that normally needed to address random material, manufacturing, testing variations
Notes: 4000, normally I may design for 4800 to cover for normal random material, manufacturing, testing variations. Now I have to add an extra 500 psi on top of that at least!
In Note 8, ASTM C31 provides some guidance on methods that can be used to maintain the moisture and temperature environment for the initial curing of test specimens
These are suggestions for maintaining a satisfactory moisture environment.

## Slide 30: Business Case for Improving Initial Curing
    Producer can target lower average strengths
      Less CM content, paste volume – less cracking
    Better durability
    Improved sustainability – about 10% lower embodied carbon
    Minimize low strength investigations to only genuine situations
    Less delays, lower costs and disputes
    Foster a better partnering environment
    Increase confidence in concrete construction
    Maintain competitiveness
Notes: In Note 8, ASTM C31 provides some guidance on methods that can be used to maintain the moisture and temperature environment for the initial curing of test specimens
These are suggestions for maintaining a satisfactory moisture environment.

## Slide 31: Responsibilities for Testing
ACI 301
1.7.2.2(a) Provide Owner’s testing agency with access to project site or to source of materials to perform testing and inspection activities and assist Owner’s testing agency in obtaining and handling samples at project site or at source of materials.
1.7.2 Quality control: Duties and responsibilities of Contractor
1.7.2.2(c) Provide secure location and sources of water
and electrical power on project site acceptable to Owner’s
testing agency for initial curing of concrete strength test
specimens as required by ASTM C31/C31M.
Notes: So the question often arises is who is reponsible for various factors associated with care of test specimens.
ACI 301 clearly states the contractor responsibility is to provide space and power for the initial curing of test specimens and this makes sense because the contractor has responsibility over the construction site.

## Slide 32: Responsibilities for Testing
ACI 301
1.7.3 Quality assurance: Duties and responsibilities of
Owner’s testing agency
Sampled concrete used to mold strength test specimens
(ASTM C31/C31M) will be tested for slump (ASTM C143/
C143M) or slump flow (ASTM C1611/C1611M), air content
(ASTM C231/C231M or ASTM C173/C173M), temperature
(ASTM C1064/C1064M), and density (ASTM C138/
C138M).
1.7.3.3(e) Owner’s testing agency will conduct concrete
strength tests by making and standard curing test specimens
in accordance with ASTM C31/C31M and testing them
according to ASTM C39/C39M.
Notes: In ACI 301, several responsibilities of the testing agency are addressed. It indicates that several fresh concrete tests should be performed when strength test specimens are made. This is useful background information. It also indicates that density of fresh concrete should be measured. This is also stated in ASTM C94. Density is a useful test that can provide additional information to evaluate low strength test results – such as excessive air or water in the concrete.
ACI 301 also indicates that it is responsibility of the testing agency to test cylinders in accordance with C31. This means that they are responsible to ensure specimens are maintained within the temperature and moisture requirements of standard curing during the initial curing period in C31. Some concrete producers, testing agencies, and contractors partner to build a curing shed or box. Improper testing can lead to low break investigations, and coring that can cause delays and increase project costs. This is not in the best interests of any of the stakeholders including the owners.

## Slide 33: Responsibilities for Testing
2.5.1 Initial curing—Owner or Owner’s representative will provide and maintain adequate facilities on the project site for initial storage and curing of the concrete specimens, unless otherwise specified. Specimens shall be stored under conditions that meet the requirements of ASTM C31 and shall be verified by Testing Agency. Such storage shall have temperature controls to maintain ASTM C31 temperature requirements. Calibrated temperature recording devices shall be used to record daily maximum and minimum temperatures of the initial curing environment.
Notes: ACI 311 is a specification for testing services. It says similar things like in ACI 301 and 318. But it seems to suggest that the owner has to provide the facilities for curing of test specimens and the agency will only verify that requirements of C31 were met. This differs from ACI 301.
The report section of this specification does state that the max/min temps during the initial curing period should be reported.
This specification also indicates that the distribution of reports should to all stakeholders.

## Slide 34: ACI Requirements on Initial Curing
Standard cured in accordance with ASTM C31
Contractor shall provide space and electrical power for initial curing
Testing agency shall verify standard curing is according to ASTM C31
Testing agency shall ensure that test report includes information about the initial curing period
Who is responsible for supplying the curing container on site?
  ACI 301 implies that testing agency is responsible
  ACI 311.6 states owner or Owner’s representative shall provide this
  ACI 132 A/E defines responsibilities in contract docs. Testing agency includes cost of curing container in their bid
Notes: ACI 318-19, Provision 26.12.3.1; 301-16, Provision 1.6.3.2(e)13; and 311.6-09, Provision 2.5.114, all require that specimens for acceptance testing be standard-cured in accordance with ASTM C31/C31M.
The reporting section of ASTM C31/C31M requires the agency making the specimens to report the maximum and minimum temperatures of the surrounding environment and the curing method used during initial curing. ACI 301, Provision 1.6.3.1(c), requires that the concrete strength test report includes information on storage and curing of specimens before testing, while ACI 311.6, Provision 3.3.12, requires the Testing Agency to report the maximum and minimum temperatures of the curing environment during the initial curing period to all the parties listed in the test report distribution list.
ACI 301, Provision 1.6.2.2(d), states that the Contractor is to: “Provide space and source of electrical power on project site for testing facilities acceptable to Owner’s testing agency. This is for the sole use of Owner’s quality assurance testing agency for initial curing of concrete strength test specimens as required by ASTM C31/C31M.” This implies that the Owner's testing agency will be responsible for initial curing. ACI 301, Provision 1.6.2.2(b), also states that it is the Contractor’s responsibility to allow the Owner's testing agency access to the project site for obtaining samples to make test specimens. ACI 301 defines the Contractor as “the person, firm, or entity under contract for construction of the Work.”
ACI 311.6, Section 2.5.1, states that the Testing Agency is responsible for verifying that the cylinders are maintained in accordance with ASTM C31/C31M. ACI 318, ACI 301, and ACI 311.6 require that field technicians, who prepare test specimens, must have an ACI Field testing Technician Grade I certification or acceptable equivalent. Thus, it is clear that the agency making test specimens is responsible for verifying conformance to the initial curing requirements.
The controversial topic is: “Who is responsible for supplying the curing facility on site?” ACI 301, Provision 1.6.3.2(e), under the duties and responsibilities of the Owner’s testing agency, states: “Owner’s testing agency will make and standard cure the specimens in accordance with ASTM C31/C31M…” Note that this statement is provided as information to the Contractor because ACI 301 is written to the Contractor and not the Testing Agency. This explains why the word "will" is used rather than "shall". Nevertheless, this provision implies that the testing agency is responsible for the initial curing and is also responsible for providing equipment needed to comply with the temperature requirements in ASTM C31/C31M. ACI 311.6, Section 2.5.1, which is written to the Testing Agency, states: “Owner or Owner’s representative will provide and maintain adequate facilities on the project site for initial storage and curing of the concrete specimens, unless otherwise specified.” Unfortunately, there is ambiguity in this provision because the specification does not define the "Owner's representative." Some have interpreted the Owner’s representative to be the Architect/Engineer, while others have interpreted it to include the Testing Agency. According to the International Building Code (IBC)15, the Owner is responsible for hiring the Testing Agency that conducts acceptance testing. In many jurisdictions, it is considered a conflict of interest for the Contractor to hire the Testing Agency that conducts acceptance testing.

## Slide 35: Responsibility for Curing Container
Testing agency responsible for curing container
Certified technicians
  Most knowledgeable about testing
Verify C31 compliance
Test report to include info
Clear chain of custody
Discuss in pre bid meetings
Who is Watching Out for the Cylinders? CI magazine, August 2018
Notes: Onus is on testing lab to bring this up for discussion during the bidding process.
The CI article concluded that
ACI 311.6, ACI 132R, AIA MasterSpec and project specifications should state explicitly that the Testing Agency is responsible for providing the on-site curing facility (container) and verifying that test specimens are maintained in accordance with ASTM C31/C31M at the jobsite.
Discussion: ACI 311.6 states that the Testing Agency is responsible for verifying that the specimens are stored under conditions in accordance with ASTM C31/C31M. ACI 318, ACI 301, and ACI 311.6 require that field technicians be certified. Among the project stakeholders, the Testing Agency is expected to have the most knowledge of the requirements for preparing and curing test specimens. This requirement will ensure an unambiguous chain of custody of standard-cured test specimens. This requirement should not preclude the Testing Agency from procuring the facility from the Contractor, but the Testing Agency is responsible for ensuring that test specimens are stored at temperatures conforming to ASTM C31/C31M.
ACI 301 and 311.6 require that the concrete test report includes information about the initial curing period, such as maximum and minimum temperatures of the medium surrounding the specimens. Specifiers should insist on receiving documentation of initial curing conditions. Producers can also request permission to place continuous temperature monitoring devices within the initial curing facility for independent measurements.
The AIA MasterSpec and project specifications should state explicitly that the Contractor is responsible for providing secured space, electrical power, and access for initial curing of test specimens.
Discussion: ACI 301 requires the Contractor to provide space and electrical power for initial curing by the Owner’s Testing Agency.

## Slide 36: Initial Curing Options
Notes: Some of the means used for initial curing of jobsites – from 5-gallon buckets, larger water containers, wooden curing boxes, coolers, and temperature-controlled curing boxes. The temperature should be monitored in enclosed spaces. Temperatures can get very high in wooden curing boxes and coolers. Water immersion is the preferred method

## Slide 37: Using Sand
Notes: Some use sand. The test cylinders are placed in a bucket, the bucket is filled with sand. The sand is soaked with water and the bucket is kept in a location away from sunlight and potential disturbance.

## Slide 38: Immerse in Water / Coolers
Add water (use ice if needed) and insert hi-low thermometer
Notes: Some examples of immersion in water and use of a cooler. Ice can be used to control temperature in hot weather – more easier to do this when cylinders are immersed in water.

## Slide 39: Temperature Controlled
Notes: Some testing agencies use these temperature controlled coolers. These cost more but provide the required temperature and moisture control. One concern is the potential for theft and vandalism as these systems can be expensive.

## Slide 40: Logger Info & Examples
Producers can request permission to use them in projects
Prices from $25 to $200 +
1 channel to 4+ channels
Memory – length of recording
Waterproof
USB, Bluetooth, Wi-Fi
Notes: In some projects, the concrete producer has obtained permission to place continuous temperature monitoring devices within the on-site initial-curing facility. These temperature monitoring devices are low cost, can be reused, and allow wireless data transfer to a cell phone, tablet, or computer. Producers have reported acceptable initial curing practices on those projects.

## Slide 41: MasterSpec June 2023 Version
Test lab provides curing facility for acceptance testing and verify compliance with ASTM C31
Test lab to report results to Owner, Architect, Contractor and concrete manufacturer within 48 hours.
Test reports to include curing method and maximum and minimum temperatures during initial curing period.
Testing Agency qualified in accordance with ASTM C1077, ASTM E329
Field tests - ACI Concrete Field Testing Technician, Grade I.
Laboratory tests - ACI Concrete Strength Testing Technician and Concrete Laboratory Testing Technician, Levl 1. Laboratory supervisor – ACI Concrete Laboratory Testing Technician, Level 2I.
Contractor provides daily access, secure space for storage, initial curing, and field curing of test samples, source of water and continuous electrical power at project site
Pre-installation conference requires review of initial curing
Notes: ESSENTIAL THAT THESE ARE ENFORCED IN PROJECTS THROUGH SPECS AND CONTRACTS!
Testing agency shall be responsible for providing curing container for composite samples on Site and verifying that field-cured composite samples are cured in accordance with ASTM C31//C31M.
Testing agency shall immediately report to Architect, Contractor and concrete manufacturer any failure of Work to comply with Contract Documents.
Testing agency shall report results of tests and inspections, in writing, to Owner, Architect, Contractor and concrete manufacturer within 48 hours of inspections and tests. Test reports shall include reporting requirements of ASTM C31/C31M, ASTM C39 and ACI 301, including the following as applicable to each test and inspection:
  Information on storage and curing of samples before testing, including curing method and maximum and minimum temperatures during initial curing period.
Personnel performing laboratory tests shall be an ACI-certified Concrete Strength Testing Technician and Concrete Laboratory Testing Technician, Grade I. Testing agency laboratory supervisor shall be an ACI-certified Concrete Laboratory Testing Technician, Grade II.
Field Quality Control Testing Agency Qualifications: An independent agency qualified in accordance with ASTM C1077 and ASTM E329 for testing indicated.
Personnel conducting field tests shall be qualified as an ACI Concrete Field Testing Technician, Grade I, in accordance with ACI CPP 610.1 or an equivalent certification program.
Instructions to Contractor: Provide reasonable auxiliary services to accommodate field testing and inspections, acceptable to testing agency, including the following:
  Daily access to the Work
  Incidental labor and facilities necessary to facilitate tests and inspections
  Secure space for storage, initial curing, and field curing of test samples, including source of water and continuous electrical power at project site during site curing period for test samples
  Security and protection for test samples and for testing and inspection equipment at Project site
Pre-installation conference now requires the review of the initial curing and field curing of field test cylinders (ASTM C31/C31M)

## Slide 42: Review of a Test Report
Reporting requirements of C31 and C39
Dates – pour, cylinders made, rec’d at lab
Ambient / concrete temperature
Slump, air content, density
Duration of initial curing
Min / max temperatures
Curing method
7 & 28 day strengths
  Strength gain
Notes: Attention to details is extremely important when reviewing a test report of compression test results. A concrete producer should maintain a record of test results in the sequence of the date made and record all the pertinent information relative to these results.
Ensure that all reports have a date of pour. Often, test cylinder information is misleading due to improper reporting of the date.
Ambient temperatures are of great importance especially when curing is non-standard.
Make sure proper test dates are reported.
All cylinder tests should have slump, air & temperature data.
The time the cylinders were removed from the job and transported to the lab is needed to confirm initial curing duration.
Each concrete mixture has a unique rate of strength gain between 7 and 28 days. It is not a constant percentage. The producer can check that this strength gain reported by the testing lab is consistent with what they know about that concrete mixture.

## Slide 43
Notes: This is an example of a test report that shows some issues. The specified strength is 5000 psi at 28 days.
It is a hot day – the ambient temperature is 89F, the concrete temperature is 92 F. So conditions are not too good for the initial curing.
The cylinders were cast on Sept 12 and received at the lab on the 16 – a difference of 3 to 4 days that does not conform to ASTM C31.
The sample was obtained from a 2 yd load. This should be avoided. Test samples should be obtained from larger load sizes – close to mixer capacity.
The lab indicates that it has complied with ASTM C31. But there is no record of max and min temps nor curing method during the initial curing at the jobsite.
The lab flagged this report because the one cylinder tested at 7-days was low. 1 cylinder is not a test result. There is no 7 day requirement; the rate of strength gain is unknown, so there is no basis to flag this.

## Slide 44: Evaluating Test Results
What do Standards Say
Responsibilities
Reporting
Data evaluation
  Precision
  Rating test results
Notes: This Technology in Practice sheet (TIP 16) discusses various details that can be useful when troubleshooting or evaluating strength test results. It discusses these topics and provides numerical examples.
Some of the details on evaluation of strength test results that is covered in this TIP are summarized in the next few slides.

## Slide 45: Testing variability (ACI 214R)
Within-batch coefficient of Variation (V1)
Average range ( ) from10 tests
= Average strength
No. Specimens | d2
2 | 1.128
3 | 1.693
4 | 2.059
Notes: ACI 214R describes a procedure to evaluate variability associated with testing by calculating the within-batch variability. This is sometimes referred to as the within-test or single operator variability.
Variability due to testing is estimated by the within-batch coefficient of variation (V1) calculated based on the average range (difference between maximum and minimum) in strengths of companion (replicate) cylinders comprising a strength test result which are cast from the same composite sample of concrete tested at the same age using Equation 1. Since the cylinders are made from the same concrete sample the material and manufacturing variability are assumed to be negligible and the strength difference between the cylinders is assumed as due to testing variability.
Average range should be calculated from at least 10 strength test results. The factor d2 is used to estimate the standard deviation, s1 from the average range and depends on the number of cylinders used
The within-batch coefficient of variation (V1), in percent, is determined from standard deviation, s1, estimated from the average range, and the average strength.

## Slide 46: Example Calculation of V1
Cylinder 1, psi | Cylinder 2, psi | Strength Test Result, psi | Range, psi
6740 | 7120 | 6930 | 380
7050 | 6750 | 6900 | 300
5640 | 5830 | 5735 | 190
5570 | 5550 | 5560 | 20
6030 | 5700 | 5865 | 330
5690 | 5650 | 5670 | 40
5530 | 5600 | 5565 | 70
5350 | 5320 | 5335 | 30
4650 | 5080 | 4865 | 430
5800 | 6080 | 5940 | 280
Average |  | 5837 | 207
Notes: This is a numerical example of calculating the component of variation associated with testing. This set of data uses 2 cylinders for each test result.
V1 is calculated from range which is based on companion cylinders. Note that 10 test results are being used
The variation from this set of data is estimated to be 3.2%.

## Slide 47: Within-batch precision
Quality Standards (ACI 214) | Excellent | Very Good | Good | Fair | Poor
V1, % | < 3.0 | 3.0 to 4.0 | 4.0 to 5.0 | 5.0 to 6.0 | > 6.0
Average Range of 2 Companion Cylinders (assuming avg. 4800 psi) | < 162 | 162 to 217 | 217 to 271 | 271 to 325 | > 325
V1 > 6% - reason to question testing
V1 between 4 and 6% - potential problems
V1 between 2 and 3% - C39 testing variation
< 1.5% - likely too good to be true
Notes: ACI 214R indicates quality standards for testing based on the measured within-batch coefficient of variation V1
The associated average range range (R) of 2 companion cylinders, assuming an average strength level of 4800 psi (33 MPa) is included in the table.
To compare testing variation for different strength levels use V1 as opposed to the average range.
To track V1, concrete test reports need to report the strength of individual cylinders. The concrete producer inputs the results in a spreadsheet to calculate V1 based on the last 10 strength test
If V1 is between 4% and 6%, there are potential problems, and if V1 is above 6%, the testing should be questioned.
For reasonably good testing V1 should be in the range of 2 to 3% due to expected variation in the ASTM C39 compressive strength test method.
If it is a very low value, there may be cause to question whether cylinders are being tested to complete failure or if both cylinders are actually being tested.

## Slide 48: ASTM C39 Single Operator precision
Companion cylinders tested at same age
Acceptable range should not be exceeded more often than 1 time in 20
Notes: Another method to evaluate testing is to use the Within-Test Precision of ASTM C39.
the within-test precision is derived from tests of 6 by 12 in. and 4 by 8 in. cylinders made from a well-mixed sample of concrete under laboratory conditions and under field conditions.
The acceptable range between two or three cylinders in the field or the lab can be used. The acceptable range should not be exceeded very often – one time in 20 is a 5% occurrence that is considered acceptable.

## Slide 49: Example Calculation within-batch Range
Cylinder 1, psi | Cylinder 2, psi | Test Result, psi | Range, psi | Range, %
6740 | 7120 | 6930 | 380 | 5.5%
7050 | 6750 | 6900 | 300 | 4.3%
5640 | 5830 | 5735 | 190 | 3.3%
5570 | 5550 | 5560 | 20 | 0.4%
6030 | 5700 | 5865 | 330 | 5.6%
5690 | 5650 | 5670 | 40 | 0.7%
5530 | 5600 | 5565 | 70 | 1.3%
5350 | 5320 | 5335 | 30 | 0.6%
4650 | 5080 | 4865 | 430 | 8.8%
5800 | 6080 | 5940 | 280 | 4.7%
Average |  | 5837 | 207 | 
Notes: In this set of 10 data points with 2 cylinders, the range exceeds 8% once. So this may not be a reason to question the quality of testing.

## Slide 50: Example Calculation - within batch Range
No. | Cylinder 1 | Cylinder 2 | Test Result | Within-batch range | Within-batch range, % | Moving Average of 10 Tests | Moving average of 10 Ranges | Moving 10 test V1, %
1 | 4498 | 4254 | 4376 | 244 | 5.6% |  |  | 
2 | 4318 | 3842 | 4080 | 476 | 11.7% |  |  | 
3 | 3782 | 3674 | 3728 | 108 | 2.9% |  |  | 
4 | 3527 | 3263 | 3395 | 264 | 7.8% |  |  | 
5 | 4571 | 3969 | 4270 | 602 | 14.1% |  |  | 
6 | 4543 | 5415 | 4979 | 872 | 17.5% |  |  | 
7 | 3988 | 4172 | 4080 | 184 | 4.5% |  |  | 
8 | 3361 | 3339 | 3350 | 22 | 0.7% |  |  | 
9 | 4831 | 4807 | 4819 | 24 | 0.5% |  |  | 
10 | 3411 | 3315 | 3363 | 96 | 2.9% | 4044 | 289 | 289/(1.128X4044)=6.3%
11 | 3619 | 3913 | 3766 | 294 | 7.8% | 3983 | 294 | 6.5%
12 | 3880 | 4082 | 3981 | 202 | 5.1% | 3973 | 267 | 5.9%
Notes: In this set of data, the Range is exceeded 3 times in 12 points (25%of the time). C39 precision statement says only 1 in 20 (5%) chances of this happening so clearly that is a violation
Also V1 calculated is high - at or higher than 6%. SO there is a concern with the quality of this testing. Note that last 10 test results are being used for V1 calculation. So, we don’t have any entry for the first 9 test results. Further, it is a moving 10 test V1.

## Slide 51: Control Charts to Monitor Testing
Notes: These are two types of plots monitoring the quality of testing. The figure on the left plots the range of the two cylinders prepared from the same concrete sample expressed as a percent of the average strength. For this
the control limit for acceptable range of two cylinders uses the C39 precision statement of 8% (appropriate for 6x12s for 4x8s since 3 cylinders are used it should be 11%, use 9% if only 2 4x8 cylinders are tested). The range of 8% is exceeded more often than 1 in 20, suggesting that cylinder fabrication and testing techniques need to be reviewed.
In the right hand figure the moving 10 test within-batch coefficient of variation (V1) in percent is plotted relative to the ACI 214R categories for testing variation. . For this example also, the testing quality is poor most of the time.

## Slide 52: Evaluating Strength Data
Poor initial curing will reduce strength
But may not reflect within batch variation
Notes: The analysis of strength data from companion cylinders to determine range or V1 may not capture improper testing. If sampling and testing procedures are deficient - initial and final curing, capping material, testing-machine
calibration, etc. - these would affect companion cylinders from the same sample equally and may not increase V1 but will still result in lower measured strengths and impact the standard deviation of strength test results. Job-site conditions (temperature, humidity) and practices vary every day; therefore, cylinders cast at different time periods are expected to experience different initial curing conditions if not subject to standard curing. However, companion cylinders cast from the same batch of concrete should experience identical initial uring conditions. In summary, variations in initial curing conditions are unlikely to influence the range of compressive strength of companion cylinders prepared from a batch but will impact the batch-to-batch variation and therefore the overall strength variability.

## Slide 53: ASTM C39 Multi-lab precision
COV = 5%
Acceptable difference between 2 = 14%
Useful for companion testing
Same sample tested by 2 labs at same age
  Split samples (same wheelbarrow or same load)
Notes: Another thing that can be useful is to perform companion testing with the laboratory of record. This is sometimes done on large projects or when there have been problems with testing. ASTM C39 has a Multilaboratory Precision statement that can be useful in determining whether two sets of results performed by different laboratories are significantly different (statistically based).
Ideally companion testing should be done on a split sample – the test specimens for each lab should be prepared from the same concrete sample. Sometimes this is not possible, but testing concrete from the same load is also possible. Alternatively, a poplulation of data tested by two labs can be compared to observe differences in overall average.
The ASTM C39 multilaboratory precision says that the difference in test results between two labs testing the same concrete should not exceed 14% of the average more often than 1 time in 20.

## Slide 54: Companion Tests
Chart: Companion Strength Test Data
| 41393 | 41393 | 41393 | 41393 | 41393 | 41395 | 41395 | 41403 | 41403 | 41407 | 41407 | 41409 | 41409 | 41409 | 41409 | 41409 | 41410 | 41410 | 41417 | 41417 | 41417 | 41417 | 41417 | 41417 | 41417 | 41424 | 41428 | 41428 | 41428 | 41428
Test Lab | 6405 | 5010 | 5330 | 5010 | 4830 | 5850 | 5590 | 4930 | 5210 | 4930 | 4870 | 4970 | 4380 | 4530 | 4435 | 4180 | 5250 | 4300 | 5410 | 4950 | 5130 | 4750 | 4910 | 5150 | 5270 | 4140 | 4970 | 5230 | 5305 | 4990
Company | 6425 | 6460 | 6125 | 6595 | 7520 | 6860 | 6825 | 6405 | 7505 | 7065 | 6705 | 6050 | 6570 | 6255 | 6035 | 6330 | 6510 | 7015 | 6320 | 6260
Lab Avg | 5007.1667 | 5007.1667
Comp Avg | 6591.75 | 6591.75
Company Data at plant; Lab data at jobsite
Specimens from the same sample are better to evaluate for multi-lab precision
Notes: This is a series of test data comparing tests done by the laboratory of record and the concrete producer. In this case, split sample testing was not possible. The producer obtained samples at the plant, the testing agency at the jobsite. The loads tested were different. There could have been some modifications to the loads before concrete was discharged at the jobsite.
However, the plot indicates a distinct difference in the averages between the two sets of test results. The average difference is about 1600 psi. and all the testing lab results are lower than those made and tested by the concrete producer.

## Slide 55: Importance of Good Testing
Strength Standard Deviation (variability)
  Materials
  Production
  Testing
Components of variation are cumulative
Reducing Testing Variation helps isolate other causes of variation that the producer can control
Notes: The significance of testing is important to the overall quality of the project.
The components of variation associated with strength test results can be broadly attributed to materials, production and testing. The components of variation are cumulative. Thus if the component of variation associated with testing is large, the variation that the producer needs to control (materials and production) through his quality control activities become difficult to isolate. Further, this increases the variation of the strength test results that is not representative of what the producer is doing. This inflates the standard deviation and will require a higher level of over-design for strength that increases the materials cost to the concrete producer.

## Slide 56: What if you have Low Test Results?
NRMCA Pub 133
  Confirm likelihood of low strength
    Verify testing accuracy
    Non destructive tests
  Structural capacity reduced (Engineer decision)?
  Core tests
  Load tests
  Corrective measures
Establish responsibility (monetary) for low strength evaluations (pre-construction)
Notes: When there are low strength results, this results in some evaluation that will delay and add costs to participants on a project including the contractor and the owner.
NRMCA Publication 133 recommends a sequence of steps that should be followed. The first step is to evaluate whether the low strength results can be confirmed – by evaluating data and practices and follow that by non-destructive tests.
The next step is to establish (by design calculations) whether the low strength impacts the structural capacity in that portion of the structure. Its possible that the specified strength level is not required.
The ACI 318 has provisions for strength tests of cores.
Load tests can be used to determine structural capacity etc. This is covered in ACI 318.
Corrective measures may be retrofitting the structure to increase its load carrying capacity or to remove and replace. This will generally cost much more than it cost to construct the structure in the first place.
If low strength results can be attributed to the responsible party, then it is appropriate that the cost for the evaluation is borne by this entity. These aspects should be established in a pre-construction meeting.

## Slide 57: Testing Concrete Cores
ACI 318 criteria:
  Average of 3 cores ≥ 0.85  c
  Individual core ≥ 0.75  c
Notes: When cores are tested for the purpose of investigation of low strength test results, the cores should be obtained, preconditioned and tested according to the provisions of ASTM C 42. The ACI 318 Building code indicates that
Concrete in an area represented by core tests shall be considered structurally adequate if
The average of three cores is equal or greater than 85% of ´c.
No single core should test less than 75% of ´c.

## Slide 58: Improving Quality of Testing
www.nrmca.org/quality
Notes: This Technology in Practice sheet (TIP 16) discusses various details that can be useful when troubleshooting or evaluating strength test results. It discusses these topics and provides numerical examples.
Some of the details on evaluation of strength test results that is covered in this TIP are summarized in the next few slides.

## Slide 59: Summary
ACI Standards, AIA MasterSpec
  Defines acceptance criteria for strength test results
  Laboratories should conform to ASTM C1077
  Technicians in the field and lab should be certified
  Initial curing in accordance with ASTM C31
    Max-min temps and curing method must be recorded (and reported)
    Testing agencies responsible for curing container for specimens onsite
  Test reports should be distributed to all stakeholders
  Criteria for core tests are defined
Testing variation is high when
  V1>4% (from last 10 data points)
  Range >8% (or C39) more than 1-in-20
Responsibility for low strength evaluation defined
Notes: Industry standards are clear and consistent on testing concrete and acceptance criteria. The qualifications of inspectors and testing agencies are stated. The details regarding testing are clearly stated. There are ways to evaluate whether testing has been performed in accordance with the standards.
It is incumbent on a testing agency to ensure that testing of concrete is reliable and provides assurance that the these results are appropriate to ensure compliance with the contract.
The responsibility for low strength test results can be either due to the quality of the concrete or the quality of the testing. The responsible party for low strengths should be liable for associated costs for evaluation and recourse.

## Slide 60: Code and Standard Requirements on Concrete Testing
Questions